Enhancement of the production of bio-aromatics from bamboo pyrolysis: wet torrefaction pretreatment coupled with catalytic fast pyrolysis

Zhouyang Hua＃, Liang Zhua＃, Ming Huanga, Jie Lia, Bo Caia, Dengyu Chenb, Lingjun Zhuc, Youyou Yangd*, Zhongqing Maa*

aCollege of Chemistry and Materials Engineering, Zhejiang A & F University, Hangzhou, Zhejiang 311300, China

bCollege of Materials Science and Engineering, Nanjing Forestry University, Nanjing City, Jiangsu Province, 210037, China

cState Key Laboratory of Clean Energy Utilization, Zhejiang University, Hangzhou, Zhejiang 310027, China

dCollege of Humanities and Law, Zhejiang A & F University, Hangzhou, Zhejiang 311300, China

Corresponding author: yangyy@zafu.edu.cn (Youyou Yang) and mazq@zafu.edu.cn (Zhongqing Ma)

First author: Zhouyang Hu＃and Liang Zhu＃, these two authors contributed equally to this work.

Postal address: College of Chemistry and Materials Engineering, Zhejiang A & F University, 666 Wusu Road, Hangzhou City, Zhejiang Province, 311300, China

Telephone: +86-571-6110-0905; Fax: +86-571-6110-0905

## 2.3. Basic properties of the raw and wet torrefied bamboo

The proximate analysis, ultimate analysis, and calorific value of the raw and wet torrefied bamboo were determined by the automatic proximate analyzer (YHGF-8000A, Hebi Yinghua Instrument Co., Ltd., China), the elemental analyzer (Vario EL III, Elementary, Germany), and the automatic calorimeter (ZDHW-8, Hebi Hengfeng Coal Analysis Equipment Co., Ltd., China), respectively. The contents of inorganic element, especially the alkali and alkaline earth metals (K, Na, Ca, and Mg), were tested by the inductively coupled plasma-optical emission spectrometer (ICP-OES 730, Agilent, USA). In this test, 0.50 g sample was added to the Teflon crucible, then was digested in the HNO3: HCl: H2O2 (8:1:1 v/v) solution using microwave (Multiwave 3000, Anton Parr). After that, the solution was diluted with purified water to 50 ml for the ICP-OES analysis.

The chemical functional group of the raw and wet torrefied bamboo was tested by using the fourier transform infrared spectrometry (Nicolet 6700, Thermo Fisher Scientific, USA). During this test, the mass ratio of feedstock-to-KBr was 200. The resolution and the spectral region were 4 cm-1 and 4000 to 500 cm-1, respectively. The crystallinity of the raw and wet torrefied bamboo was determined by using the X-ray diffractometer (XRD 6000, Shimadzu, Japan). The pyrolysis behaviors of the raw and wet torrefied bamboo was performed by the thermogravimetric analyzer (TG209F1 Libra, Netzsch, Germany). The pyrolysis temperature was raised from room temperature to 800 ºC at a heating rate of 10 ºC/min. The flow rates of the carrier gas (high-purity N2, 99.999%) and protective gas (high-purity N2, 99.999%) were 40 ml/min and 20 ml/min, respectively.

Table S1. Effect of WTP temperature on the compound distribution in bio-oil (CFP temperature = 850 ºC, catalyst = HZSM-5 (25), catalyst-to-biomass mass ratio = 3:1)

| Substance | Category | Compounds | Absolute peak area (x 107 a.u./mg) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Raw | 180 ºC | 200 ºC | 220 ºC | 240 ºC | 260 ºC |
| Aromatics | MAHs | Benzene | 1.89 | 2.33 | 2.77 | 3.34 | 2.47 | 2.11 |
|  |  | Toluene | 2.22 | 3.13 | 5.55 | 6.50 | 5.98 | 5.60 |
|  |  | Xylene | 2.71 | 5.14 | 5.52 | 6.43 | 5.62 | 4.19 |
|  |  | Ethylbenzene | 0.31 | N.D. | N.D. | N.D. | 0.75 | N.D. |
|  |  | Benzene, 1-ethyl-2-methyl- | 0.73 | 0.91 | 0.90 | 0.70 | 0.85 | 0.53 |
|  |  | Benzene, 1,2-diethyl- | N.D. | 0.07 | 0.10 | N.D. | 0.13 | 0.33 |
|  |  | Benzene, propyl- | N.D. | N.D. | 0.07 | N.D. | 0.66 | N.D. |
|  |  | Styrene | N.D. | N.D. | 0.02 | N.D. | N.D. | N.D. |
|  |  | Benzene, 1-ethenyl-3-methyl- | 0.02 | 0.50 | 0.40 | 0.54 | 0.16 | N.D. |
|  |  | Benzene, 1,2,3-trimethyl- | N.D. | 0.19 | 0.13 | 0.20 | 0.23 | 0.12 |
|  |  | Benzene, 1-propynyl- | N.D. | N.D. | 0.07 | N.D. | N.D. | 0.12 |
|  |  | Benzene, 1-methyl-4-(2-propenyl)- | N.D. | N.D. | N.D. | 0.21 | 0.07 | 0.91 |
|  |  | 1-Phenyl-1-butene | N.D. | N.D. | 0.19 | N.D. | 0.09 | N.D. |
|  |  | 3-Methylphenylacetylene | 0.90 | N.D. | N.D. | 0.97 | N.D. | N.D. |
|  |  | 2,4-Dimethylstyrene | 0.06 | 0.10 | N.D. | N.D. | N.D. | N.D. |
|  |  | Indene | N.D． | 1.22 | N.D. | N.D. | N.D. | 0.47 |
|  |  | 1H-Indene, 3-methyl- | 0.32 | 0.20 | 0.13 | N.D. | 0.43 | 0.38 |
|  |  | Naphthalene,1,2-dihydro- | 0.08 | 0.40 | 0.31 | 0.72 | N.D. | N.D. |
|  |  | Naphthalene,1,2-dihydro-3-methyl- | N.D. | 0.02 | 0.07 | 0.19 | 0.05 | N.D. |
|  |  | Subtotal | 9.25 | 14.23 | 18.38 | 19.90 | 17.47 | 14.76 |
|  | PAHs | Naphthalene | 1.90 | 2.06 | 2.77 | 1.50 | 2.86 | 2.46 |
|  |  | Naphthalene, 2-methyl- | 0.81 | 3.07 | 2.18 | 2.66 | 1.74 | 1.91 |
|  |  | Naphthalene, 2-ethyl- | N.D. | 0.05 | N.D. | 0.09 | N.D. | N.D. |
|  |  | Naphthalene,1,3-dimethyl- | 0.20 | 0.45 | 0.47 | 0.67 | 0.47 | 0.30 |
|  |  | Biphenyl | 0.05 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | Fluorene | 0.05 | 0.07 | 0.06 | 0.13 | N.D. | 0.05 |
|  |  | Phenanthrene | N.D. | N.D. | 0.38 | 0.36 | N.D. | 0.12 |
|  |  | Phenanthrene, 1-methyl- | 0.03 | 0.08 | 0.12 | N.D. | N.D. | N.D. |
|  |  | Anthracene | 0.06 | 0.41 | N.D. | N.D. | N.D. | N.D. |
|  |  | Anthracene, 1-methyl- | 0.02 | 0.04 | N.D. | N.D. | 0.07 | 0.06 |
|  |  | 1H-Cyclopropa[l]phenanthrene, 1a,9b-dihydro- | N.D. | N.D. | N.D. | 0.18 | N.D. | N.D. |
|  |  | Diphenylacetylene | N.D. | N.D. | N.D. | N.D. | 0.07 | N.D. |
|  |  | Subtotal | 3.68 | 6.23 | 5.99 | 5.57 | 5.21 | 4.91 |
|  |  | Total | 12.94 | 20.46 | 24.38 | 25.46 | 22.68 | 19.67 |
| Aliphatics | Alkanes | Heptacosane | 4.87 | 3.95 | 1.84 | 1.62 | 1.67 | 2.98 |
|  |  | Butane, 2-methyl- | 0.06 | 0.08 | 0.05 | N.D. | N.D. | N.D. |
|  |  | n-Hexane | N.D. | N.D. | 0.21 | N.D. | 0.13 | 0.08 |
|  |  | Octacosane | N.D. | N.D. | 1.06 | 0.62 | 1.43 | N.D. |
|  |  | Cyclopropane,(1,2dimethylpropyl)- | N.D. | N.D. | N.D. | N.D. | 0.06 | 0.03 |
|  |  | Pentane, 2-methyl- | N.D. | N.D. | N.D. | N.D. | N.D. | 0.05 |
|  |  | Subtotal | 4.93 | 4.04 | 3.16 | 2.24 | 3.23 | 3.34 |
|  | Olefins | 2-Butene | 0.22 | 0.45 | 0.74 | 0.59 | 0.15 | 0.09 |
|  |  | Butane, 2-methyl- | N.D. | N.D. | N.D. | N.D. | 0.40 | N.D. |
|  |  | 1,3-Cyclopentadiene | 0.19 | 0.16 | N.D. | 0.74 | 0.22 | N.D. |
|  |  | 1,3-Pentadiene | N.D. | N.D. | 0.07 | N.D. | 0.37 | 0.25 |
|  |  | 1-Penten-3-yne | N.D. | N.D. | 0.22 | N.D. | N.D. | 0.73 |
|  |  | 1-Pentene, 2-methyl- | N.D. | N.D. | N.D. | N.D. | 0.09 | N.D. |
|  |  | 1-Hexene | N.D. | N.D. | 0.12 | N.D. | 1.47 | N.D. |
|  |  | 1-Hexene, 4-methyl- | N.D. | N.D. | 2.37 | N.D. | N.D. | N.D. |
|  |  | 1,3,5-Hexatriene | 0.12 | 0.17 | 0.72 | 0.62 | 0.21 | 0.08 |
|  |  | 4-Methyl-2-pentyne | N.D. | N.D. | 0.09 | N.D. | 0.10 | N.D. |
|  |  | Cyclopentene,4,4-dimethyl- | N.D. | N.D. | 0.05 | 0.14 | 0.21 | 0.08 |
|  |  | 2,4-Dimethyl-1-heptene | N.D. | N.D. | 0.09 | N.D. | N.D. | N.D. |
|  |  | 1-Decene, 8-methyl- | N.D. | N.D. | N.D. | N.D. | 1.01 | N.D. |
|  |  | D-Limonene | 0.06 | N.D. | 0.08 | 0.08 | 0.09 | 0.02 |
|  |  | 5-Undecene, (Z)- | N.D. | N.D. | N.D. | N.D. N.D. | 0.07 | 0.05 |
|  |  | 17-Pentatriacontene | N.D. | N.D. | N.D. | N.D. | 0.18 | 0.46 |
|  |  | Squalene | 1.27 | 2.39 | N.D. | 3.56 | N.D. | 2.15 |
|  |  | Subtotal | 1.87 | 3.12 | 4.57 | 5.73 | 4.39 | 3.91 |
|  |  | Total | 6.78 | 7.16 | 7.73 | 7.97 | 7.61 | 7.15 |
| Oxygenates | Acids | n-Hexadecanoic acid | 5.46 | 3.11 | 4.03 | 1.99 | 3.62 | 2.46 |
|  |  | Octadecanoic acid | 0.38 | 0.07 | 2.34 | 0.67 | 0.47 | 0.55 |
|  |  | Oleic Acid | 0.87 | 0.08 | 0.04 | 0.17 | 0.02 | 0.15 |
|  |  | Tetradecanoic acid | N.D. | 1.31 | N.D. | N.D. | N.D. | 0.09 |
|  |  | 9-Hexadecenoic acid | N.D. | 0.50 | N.D. | 0.11 | N.D. | 0.23 |
|  |  | Erucic acid | N.D. | N.D. | 0.24 | N.D. | 0.18 | 0.18 |
|  |  | Subtotal | 6.71 | 5.71 | 6.65 | 2.94 | 4.29 | 3.67 |
|  | Alcohols | 3-Penten-1-ol | 0.81 | 4.11 | 0.74 | 0.82 | 0.05 | 0.04 |
|  |  | 1-Butanol, 2-methyl- | N.D. | 0.32 | 0.09 | 0.07 | N.D. | N.D. |
|  |  | 1-Tetradecanol | N.D. | N.D. | N.D. | N.D. | 0.28 | 0.08 |
|  |  | 2-Pentyne-1,5-diol,1,5diphenyl | N.D. | N.D. | 0.16 | N.D. | N.D. | N.D. |
|  |  | 2-Hexadecanol | 0.08 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | Ethanol, 2-(octadecyloxy)- | 0.48 | 2.10 | 0.53 | 0.36 | 0.34 | 0.13 |
|  |  | 1-Heptatriacotanol | N.D. | N.D. | 0.24 | 0.18 | N.D. | N.D. |
|  |  | Subtotal | 1.38 | 6.53 | 1.76 | 1.43 | 0.67 | 0.25 |
|  | Esters | 5,8,11-Eicosatriynoic acid, methyl ester | 0.09 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | Pentadecanoic acid, 13-methyl-, methyl ester | N.D. | N.D. | N.D. | N.D. | 0.08 | 0.08 |
|  |  | Heptadecanoic acid, 16-methyl-, methyl ester | N.D. | N.D. | N.D. | N.D. | 0.14 | 0.13 |
|  |  | 9-Hexadecenoic acid, eicosyl ester, | N.D. | 0.08 | N.D. | N.D. | N.D. | N.D. |
|  |  | Hexadecanoic acid,ethyl ester | N.D. | 0.16 | N.D. | N.D. | N.D. | N.D. |
|  |  | Octadecanoic acid,4hydroxy-, methyl ester | N.D. | 0.36 | N.D. | N.D. | N.D. | N.D. |
|  |  | Oleicacid,3-(octadecyloxy)propyl ester | 9.99 | 1.14 | 0.76 | 1.73 | 0.18 | 0.30 |
|  |  | Ethyl iso-allocholate | N.D. | N.D. | 0.05 | N.D. | N.D. | N.D. |
|  |  | Hexadecanoic acid, 2(octadecyloxy)ethyl ester | N.D. | 0.07 | N.D. | 0.37 | N.D. | 0.54 |
|  |  | Subtotal | 10.07 | 1.82 | 0.82 | 2.10 | 0.41 | 1.06 |
|  | Furans | Furan, 2-methyl- | 0.10 | 0.15 | 0.42 | 0.12 | N.D. | N.D. |
|  |  | Benzofuran, 2-methyl- | N.D. | 0.17 | N.D. | 0.11 | N.D. | N.D. |
|  |  | Subtotal | 0.10 | 0.32 | 0.42 | 0.23 | N.D. | N.D. |
|  | Phenols | p-Cresol | 1.27 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | 1-Naphthalenol, 1,2,3,4-tetrahydro-3-methyl- | 0.11 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | Subtotal | 1.39 | N.D. | N.D. | N.D. | N.D. | N.D. |
|  | Oxides | 3,4-Altrosan | N.D. | 1.25 | N.D. | 0.08 | N.D. | N.D. |
|  |  | β-D-Glucopyranose, 1,6-anhydro- | N.D. | N.D. | 2.02 | N.D. | N.D. | N.D. |
|  |  | Subtotal | N.D. | 1.25 | 2.02 | 0.08 | N.D. | N.D. |
|  |  | Total | 19.66 | 15.64 | 11.68 | 6.79 | 5.41 | 4.99 |

Table S2. Effect of different types of zeolite catalyst on the compound distribution in bio-oil (WTP temperature = 220 ºC, CFP temperature = 850 ºC, catalyst-to-biomass mass ratio = 3:1)

| Substance | Category | Compounds | Absolute peak area (x107 a.u./mg) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | MCM | USY | HY | HZSM-5(100) | HZSM-5(25) |
| Aromatics | MAHs | Benzene | 0.71 | 2.40 | 2.83 | 3.43 | 3.34 |
|  |  | Toluene | 0.80 | 3.22 | 3.24 | 6.33 | 6.50 |
|  |  | Xylene | 0.38 | 2.69 | 3.12 | 5.36 | 6.43 |
|  |  | Styrene | 0.73 | N.D. | N.D. | N.D. | N.D. |
|  |  | Benzene, 1-ethyl-3-methyl- | N.D. | 0.17 | 0.61 | 0.48 | 0.70 |
|  |  | Benzene, 1,2,3-trimethyl- | N.D. | 1.20 | 1.12 | 0.27 | 0.20 |
|  |  | Benzene, 1,2,3,4-tetramethyl- | N.D. | 0.13 | N.D. | N.D. | N.D. |
|  |  | Benzene, 1-ethenyl-3-methyl- | N.D. | N.D. | N.D. | 0.52 | 0.54 |
|  |  | Benzene, 1-methyl-4-(2-propenyl)- | N.D. | N.D. | N.D. | 0.18 | 0.21 |
|  |  | Benzene, 1,2-diethyl- | N.D. | N.D. | N.D. | 0.34 | N.D. |
|  |  | Benzene, 1-propenyl- | 0.06 | N.D. | N.D. | N.D. | N.D. |
|  |  | 3-Methylphenylacetylene | N.D. | N.D. | N.D. | N.D. | 0.97 |
|  |  | Naphthalene, 1,2-dihydro- | N.D. | N.D. | N.D. | N.D. | 0.72 |
|  |  | Naphthalene, 1,2-dihydro-3-methyl- | N.D. | N.D. | N.D. | N.D. | 0.19 |
|  |  | 1-Phenyl-1-butene | N.D. | N.D. | 0.16 | N.D. | N.D. |
|  |  | Indene | 0.12 | 0.12 | N.D. | 0.14 | N.D. |
|  |  | 1H-Indene, 3-methyl- | 0.15 | 0.27 | N.D. | 0.74 | N.D. |
|  |  | Benzocycloheptatriene | 0.17 | N.D. | N.D. | 0.21 | N.D. |
|  |  | Subtotal | 3.14 | 11.44 | 12.11 | 18.91 | 19.90 |
|  | PAHs | Naphthalene | 0.26 | 0.68 | 1.38 | 2.16 | 1.50 |
|  |  | Naphthalene, 1-methyl- | N.D. | 0.42 | 1.11 | N.D. | 2.66 |
|  |  | Naphthalene, 2-ethyl- | N.D. | N.D. | N.D. | N.D. | 0.09 |
|  |  | Naphthalene, 1,3-dimethyl- | 0.05 | 0.24 | 1.17 | 1.59 | 0.67 |
|  |  | Naphthalene, 1,6,7-trimethyl- | N.D. | 0.07 | N.D. | N.D. | N.D. |
|  |  | 1,1'-Biphenyl, 3,4-diethyl- | N.D. | N.D. | N.D. | 0.93 | N.D. |
|  |  | Fluorene | N.D. | 0.04 | N.D. | N.D. | 0.13 |
|  |  | Phenanthrene | N.D. | 0.13 | N.D. | N.D. | 0.36 |
|  |  | Pyrene | N.D. | 0.10 | N.D. | N.D. | N.D. |
|  |  | 1H-Cyclopropa[l]phenanthrene,1a,9b-dihydro- | N.D. | N.D. | N.D. | N.D. | 0.18 |
|  |  | Subtotal | 0.31 | 1.68 | 3.65 | 4.68 | 5.57 |
|  |  | Total | 3.45 | 14.50 | 14.78 | 23.58 | 25.46 |
| Aliphatics | Alkanes | Butane, 2-methyl- | N.D. | 0.39 | 0.18 | N.D. | N.D. |
|  |  | Pentane, 3-methyl- | N.D. | 0.15 | N.D. | N.D. | N.D. |
|  |  | Cyclopentane, methyl- | N.D. | 0.08 | N.D. | 0.06 | N.D. |
|  |  | Dodecane, 2,6,11-trimethyl- | 0.16 | N.D. | N.D. | N.D. | N.D. |
|  |  | Octadecane, 5-methyl- | 0.34 | N.D. | N.D. | N.D. | N.D. |
|  |  | Heptadecane, 9-hexyl- | N.D. | N.D. | N.D. | 0.12 | N.D. |
|  |  | Tetradecane, 2,6,10-trimethyl- | 0.32 | N.D. | N.D. | 0.04 | N.D. |
|  |  | Heptacosane | 4.26 | 6.03 | 4.72 | 1.26 | 1.62 |
|  |  | Octacosane | N.D. | N.D. | N.D. | N.D. | 0.62 |
|  |  | Subtotal | 5.08 | 6.65 | 4.91 | 1.49 | 2.24 |
|  | Olefins | 2-Butene | 0.61 | 1.09 | 0.60 | 0.57 | 0.59 |
|  |  | 1,3-Pentadiene | 0.29 | N.D. | N.D. | 0.05 | N.D. |
|  |  | 1,3-Cyclopentadiene | 0.30 | 0.12 | 0.13 | 0.26 | 0.74 |
|  |  | 1-Hexene | N.D. | N.D. | N.D. | 0.04 | N.D. |
|  |  | 2-Pentene, 3-methyl-, (E)- | N.D. | 0.52 | N.D. | N.D. | N.D. |
|  |  | 1,3-Pentadiene | 0.06 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1-Pentene, 2-methyl- | 0.09 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1,3,5-Hexatriene | 0.60 | 0.11 | 0.06 | 0.37 | 0.62 |
|  |  | 2-Hexene, 3-methyl-, (Z)- | N.D. | 0.07 | 0.07 | N.D. | N.D. |
|  |  | 1,3-Cyclohexadiene | 0.14 | N.D. | N.D. | 0.05 | 0.14 |
|  |  | 1,3-Pentadiene, 2,3-dimethyl- | N.D. | N.D. | N.D. | 0.05 | N.D. |
|  |  | 3-Methylenecyclohexene | N.D. | N.D. | N.D. | 0.04 | N.D. |
|  |  | D-Limonene | N.D. | N.D. | N.D. | 0.04 | 0.08 |
|  |  | 5-Undecene, (Z)- | 0.22 | N.D. | N.D. | N.D. | N.D. |
|  |  | 2-Dodecenal, (E)- | 0.09 | N.D. | N.D. | N.D. | N.D. |
|  |  | Squalene | 5.51 | 2.64 | 6.38 | 4.94 | 3.56 |
|  |  | 17-Pentatriacontene | N.D. | 0.12 | N.D. | N.D. | N.D. |
|  |  | Subtotal | 7.92 | 4.68 | 7.26 | 6.71 | 5.73 |
|  |  | Total | 13.01 | 11.33 | 11.18 | 8.19 | 7.97 |
| Oxygenates | Acids | 9-Hexadecenoic acid | 2.22 | 0.19 | 0.45 | N.D. | 0.10 |
|  |  | Tetradecanoic acid | N.D. | N.D. | 0.40 | N.D. | N.D. |
|  |  | n-Hexadecanoic acid | 1.79 | 0.68 | 0.58 | 3.14 | 1.99 |
|  |  | Oleic Acid | 0.59 | 6.36 | 5.47 | 0.12 | 0.17 |
|  |  | Octadecanoic acid | 1.56 | 0.08 | 0.36 | N.D. | 0.67 |
|  |  | Subtotal | 6.16 | 7.32 | 7.25 | 3.26 | 2.94 |
|  | Alcohols | 1-Pentanol, 2-methyl- | N.D. | 0.16 | N.D. | N.D. | N.D. |
|  |  | 1-Butanol, 2-methyl- | N.D. | N.D. | N.D. | 0.09 | 0.07 |
|  |  | 4-Penten-1-ol | N.D. | N.D. | N.D. | N.D. | 0.82 |
|  |  | 1-Tetradecanol | 0.43 | N.D. | N.D. | N.D. | N.D. |
|  |  | 2-Hexadecanol | 0.44 | 0.25 | N.D. | 0.13 | N.D. |
|  |  | Ethanol, 2-(octadecyloxy)- | 0.22 | 0.34 | 0.56 | 0.07 | 0.36 |
|  |  | 1-Heptatriacotanol | N.D. | N.D. | N.D. | 0.17 | 0.18 |
|  |  | 1-Dodecanol, 3,7,11-trimethyl- | 0.49 | N.D. | N.D. | N.D. | N.D. |
|  |  | Subtotal | 1.57 | 0.74 | 0.56 | 0.47 | 1.43 |
|  | Esters | Hexadecanoic acid, methyl ester | 0.45 | N.D. | N.D. | N.D. | N.D. |
|  |  | Formic acid, 2-phenylethyl ester | N.D. | N.D. | N.D. | 0.57 | N.D. |
|  |  | Octadecanoic acid, 4-hydroxy-, methyl ester | N.D. | N.D. | N.D. | 0.04 | N.D. |
|  |  | Hexadecanoic acid, 2-(octadecyloxy)ethyl ester | N.D. | N.D. | N.D. | N.D. | 0.38 |
|  |  | Di-n-octyl phthalate | N.D. | 0.25 | N.D. | 0.06 | N.D. |
|  |  | 1,4-Benzenedicarboxylic acid, bis(2-ethylhexyl) ester | N.D. | 0.21 | N.D. | N.D. | 0.11 |
|  |  | 9-Hexadecenoic acid, eicosyl ester, (Z)- | N.D. | N.D. | N.D. | 0.24 | N.D. |
|  |  | Heptadecanoic acid, 16-methyl-, methyl ester | 0.79 | N.D. | N.D. | N.D. | N.D. |
|  |  | Oleic acid, 3-(octadecyloxy)propyl ester | 4.99 | 0.70 | 1.13 | 0.92 | 1.62 |
|  |  | Subtotal | 6.23 | 1.16 | 1.13 | 1.83 | 2.11 |
|  | Furans | Furan | 0.90 | N.D. | N.D. | 0.96 | N.D. |
|  |  | Furan, 2-methyl- | 0.47 | 0.50 | 0.43 | 0.44 | 0.12 |
|  |  | Furan, 2,5-dimethyl- | 0.06 | N.D. | N.D. | N.D. | N.D. |
|  |  | Benzofuran, 2,3-dihydro-2-methyl- | N.D. | 0.71 | N.D. | N.D. | 0.11 |
|  |  | Subtotal | 1.43 | 1.21 | 0.43 | 1.40 | 0.23 |
|  | Phenols | Phenol, 3-ethyl-5-methyl- | N.D. | N.D. | N.D. | 0.05 | N.D. |
|  |  | Subtotal | N.D. | N.D. | N.D. | 0.05 | N.D. |
|  | Ketones | 6-Octen-2-one | N.D. | 1.27 | N.D. | N.D. | N.D. |
|  |  | Subtotal | N.D. | 1.27 | N.D. | N.D. | N.D. |
|  | Oxides | 1-Methoxy-2-methyl-3-butene | N.D. | N.D. | 1.07 | N.D. | 0.08 |
|  |  | 1-Butoxy-2-methyl-2-butene (E)- | N.D. | N.D. | 0.14 | N.D. | N.D. |
|  |  | D-Allose | N.D. | N.D. | N.D. | 2.20 | N.D. |
|  |  | Subtotal | N.D. | N.D. | 1.21 | 2.20 | 0.08 |
|  |  | Total | 15.39 | 11.70 | 10.58 | 9.22 | 6.79 |

Table S3. Effect of catalyst-to-biomass ratio on the compound distribution in bio-oil (WTP temperature = 220 ºC, CFP temperature = 850 ºC, catalyst = HZSM-5(25))

| Substance | Category | Compounds | Absolute peak area (x107 a.u./mg) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1:1 | 2:1 | 3:1 | 4:1 | 5:1 |
| Aromatics | MAHs | Benzene | 2.12 | 2.21 | 3.34 | 2.33 | 2.10 |
|  |  | Toluene | 3.29 | 4.25 | 6.50 | 5.63 | 5.16 |
|  |  | Xylene | 4.11 | 4.85 | 6.43 | 6.15 | 5.52 |
|  |  | Styrene | N.D. | N.D. | N.D. | N.D. | 1.11 |
|  |  | Benzene, 1-ethyl-3-methyl- | 1.54 | 2.50 | 0.70 | 0.35 | 0.19 |
|  |  | Benzene, 1,2,3-trimethyl- | N.D. | N.D. | 0.20 | N.D. | 0.32 |
|  |  | Ethylbenzene | N.D. | N.D. | N.D. | N.D. | 0.14 |
|  |  | Benzene, 1-ethenyl-3-methyl- | N.D. | N.D. | 0.54 | 0.50 | N.D. |
|  |  | Benzene, 1-methyl-4-(2-propenyl)- | N.D. | N.D. | 0.21 | 0.21 | 0.29 |
|  |  | Benzene, 1-propenyl- | 0.62 | 2.31 | N.D. | N.D. | N.D. |
|  |  | 3-Methylphenylacetylene | N.D. | N.D. | 0.97 | N.D. | N.D. |
|  |  | Naphthalene, 1,2-dihydro- | N.D. | 0.17 | 0.72 | 0.16 | 0.30 |
|  |  | Naphthalene, 1,2-dihydro-3-methyl- | N.D. | N.D. | 0.19 | N.D. | N.D. |
|  |  | Benzene, 1-butynyl- | N.D. | N.D. | N.D. | N.D. | 0.17 |
|  |  | Indene | N.D. | N.D. | N.D. | 0.25 | 0.81 |
|  |  | 1H-Indene, 3-methyl- | N.D. | N.D. | N.D. | 0.87 | N.D. |
|  |  | Subtotal | 11.68 | 16.30 | 19.90 | 17.06 | 16.12 |
|  | PAHs | Naphthalene | 2.34 | 2.04 | 1.50 | 2.63 | 3.98 |
|  |  | Naphthalene, 1-methyl- | 1.04 | 2.24 | 2.66 | 1.79 | 1.13 |
|  |  | Naphthalene, 2-ethyl- | N.D. | N.D. | 0.09 | 0.43 | N.D. |
|  |  | Naphthalene, 1,3-dimethyl- | N.D. | 0.16 | 0.67 | 0.26 | 0.50 |
|  |  | Biphenyl | N.D. | N.D. | N.D. | 0.07 | 0.07 |
|  |  | Phenanthrene, 1-methyl- | N.D. | N.D. | N.D. | 0.13 | N.D. |
|  |  | Acenaphthylene | N.D. | N.D. | N.D. | 0.11 | N.D. |
|  |  | 1-Isopropenylnaphthalene | N.D. | N.D. | N.D. | N.D. | 0.22 |
|  |  | Fluorene | N.D. | N.D. | 0.13 | 0.93 | 0.09 |
|  |  | Phenanthrene | N.D. | 0.13 | 0.36 | 0.11 | 0.46 |
|  |  | Anthracene | N.D. | N.D. | N.D. | 0.28 | 0.48 |
|  |  | 1H-Cyclopropa[l]phenanthrene,1a,9b-dihydro- | N.D. | N.D. | 0.18 | N.D. | N.D. |
|  |  | Subtotal | 3.38 | 4.56 | 5.57 | 6.85 | 6.94 |
|  |  | Total | 15.06 | 20.86 | 25.46 | 23.91 | 23.06 |
| Aliphatics | Alkanes | Cyclopropane, 1,2-dimethyl-, trans- | 1.11 | N.D. | N.D. | N.D. | N.D. |
|  |  | Dodecane | 0.12 | N.D. | N.D. | N.D. | N.D. |
|  |  | Tridecane | 0.12 | N.D. | N.D. | N.D. | N.D. |
|  |  | Tetradecane | 0.11 | N.D. | N.D. | N.D. | N.D. |
|  |  | Pentadecane | 0.20 | N.D. | N.D. | N.D. | N.D. |
|  |  | Heptadecane | 0.15 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1-Docosene | N.D. | N.D. | N.D. | 0.06 | N.D. |
|  |  | Heptacosane | 1.79 | 4.30 | 1.62 | 1.56 | N.D. |
|  |  | Octacosane | 0.23 | N.D. | 0.62 | N.D. | N.D. |
|  |  | Subtotal | 3.83 | 4.30 | 2.24 | 1.62 | N.D. |
|  | Olefins | 2-Butene | N.D. | N.D. | 0.59 | 0.75 | N.D. |
|  |  | 1,3-Pentadiene | 0.33 | 0.55 | N.D. | 1.26 | N.D. |
|  |  | 1-Penten-3-yne | N.D. | 0.23 | N.D. | N.D. | N.D. |
|  |  | 1-Butyne, 3-methyl- | 0.14 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1,3-Cyclopentadiene | 0.30 | N.D. | 0.74 | 1.43 | 0.14 |
|  |  | 1-Hexene | 0.23 | 0.22 | N.D. | N.D. | N.D. |
|  |  | 1,3,5-Hexatriene | 0.18 | 0.12 | 0.62 | N.D. | 2.41 |
|  |  | 3-Hydroxyphenylacetylene | N.D. | N.D. | N.D. | N.D. | 0.38 |
|  |  | 2-Hexene, 3-methyl-, (Z)- | N.D. | N.D. | N.D. | N.D. | N.D. |
|  |  | 1,3-Cyclohexadiene | 0.15 | 0.13 | 0.14 | 0.08 | N.D. |
|  |  | 1-Heptene | 0.12 | 0.14 | N.D. | 0.11 | N.D. |
|  |  | 1-Octene | 0.16 | 0.09 | N.D. | 0.08 | N.D. |
|  |  | 1,3,5,7-Cyclooctatetraene | N.D. | 0.51 | N.D. | N.D. | N.D. |
|  |  | 1-Decene | 0.46 | 0.13 | N.D. | 0.21 | N.D. |
|  |  | 2-Methylphenylacetylene | N.D. | N.D. | N.D. | 0.46 | N.D. |
|  |  | D-Limonene | N.D. | 0.09 | 0.08 | N.D. | N.D. |
|  |  | 2-Undecene, (E)- | 0.30 | 0.18 | N.D. | 0.13 | N.D. |
|  |  | 1-Dodecene | 0.15 | 0.17 | N.D. | 0.13 | N.D. |
|  |  | 1-Tridecene | 0.29 | 0.16 | N.D. | 0.13 | N.D. |
|  |  | Squalene | 0.48 | 0.22 | 3.56 | 0.24 | N.D. |
|  |  | Bicyclo[4.4.1]undeca-1,3,5,7,9-pentaene | N.D. | N.D. | N.D. | N.D. | 0.38 |
|  |  | Subtotal | 3.30 | 2.96 | 5.73 | 4.99 | 2.52 |
|  |  | Total | 7.13 | 7.25 | 7.97 | 6.61 | 6.32 |
| Oxygenates | Acids | Dodecanoic acid | 0.27 | 0.05 | N.D. | N.D. | N.D. |
|  |  | Benzoic acid, 2-(1-methylethyl)- | N.D. | N.D. | N.D. | N.D. | 0.07 |
|  |  | Undecanoic acid | N.D. | N.D. | N.D. | N.D. | 0.02 |
|  |  | 9-Hexadecenoic acid | 0.15 | 0.03 | 0.10 | N.D. | 0.01 |
|  |  | trans-13-Octadecenoic acid | N.D. | N.D. | N.D. | 0.18 | N.D. |
|  |  | n-Hexadecanoic acid | 4.63 | 7.53 | 1.99 | 3.54 | 0.11 |
|  |  | Oleic Acid | 1.41 | 0.57 | 0.17 | N.D. | N.D. |
|  |  | Octadecanoic acid | 0.77 | 0.42 | 0.67 | 0.26 | 1.52 |
|  |  | Subtotal | 7.23 | 8.61 | 2.94 | 3.89 | 1.74 |
|  | Alcohols | 4-Penten-2-ol, 3-methyl- | 1.20 | 0.21 | N.D. | N.D. | 0.59 |
|  |  | 1-Butanol, 2-methyl- | N.D. | 0.12 | 0.07 | N.D. | 0.11 |
|  |  | 4-Penten-1-ol | N.D. | N.D. | 0.82 | N.D. | N.D. |
|  |  | 3-Tetradecanol | 0.31 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1-Hexadecanol | 2.00 | 0.32 | N.D. | 0.41 | N.D. |
|  |  | n-Heptadecanol-1 | N.D. | 0.18 | N.D. | N.D. | N.D. |
|  |  | Ethanol, 2-(octadecyloxy)- | 0.11 | N.D. | 0.36 | 0.05 | 0.15 |
|  |  | 1-Heptatriacotanol | N.D. | N.D. | 0.18 | N.D. | N.D. |
|  |  | Subtotal | 1.27 | 0.82 | 1.43 | 4.64 | 0.85 |
|  | Esters | Hexadecanoic acid, methyl ester | 0.57 | 0.05 | N.D. | 0.11 | N.D. |
|  |  | Methyl stearate | 0.75 | 0.21 | N.D. | 0.16 | N.D. |
|  |  | Tetradecanoic acid, 2-phenyl-1,3-dioxan-5-yl ester | N.D. | 0.03 | N.D. | N.D. | N.D. |
|  |  | Hexadecanoic acid, 2-(octadecyloxy)ethyl ester | N.D. | 0.03 | N.D. | 0.06 | N.D. |
|  |  | Diisooctyl phthalate | N.D. | N.D. | N.D. | N.D. | 1.16 |
|  |  | Phthalic acid, isobutyl nonyl ester | N.D. | N.D. | N.D. | N.D. | 0.05 |
|  |  | 1-Propanol, 2-[2-(benzoyloxy)propoxy]-, benzoate | N.D. | N.D. | N.D. | N.D. | 1.28 |
|  |  | Oleic acid, 3-(octadecyloxy)propyl ester | N.D. | N.D. | 1.13 | N.D. | N.D. |
|  |  | Subtotal | 1.32 | 0.32 | 1.13 | 0.33 | 2.49 |
|  | Furans | Furan, 2-methyl- | 0.23 | 0.10 | 0.43 | N.D. | 0.02 |
|  |  | Benzofuran, 2,3-dihydro- | 0.46 | 0.26 | N.D. | 0.05 | N.D. |
|  |  | Dibenzofuran | N.D. | N.D. | N.D. | 0.08 | N.D. |
|  |  | Subtotal | 0.69 | 0.36 | 0.43 | 0.13 | 0.02 |
|  | Phenols | Phenol | 0.40 | 0.45 | N.D. | 0.32 | N.D. |
|  |  | Phenol, 2-methyl- | 0.19 | 0.31 | N.D. | 0.12 | 0.05 |
|  |  | p-Cresol | 0.63 | 0.19 | N.D. | 0.35 | N.D. |
|  |  | Phenol, 4-ethyl- | 2.85 | 0.17 | N.D. | 0.08 | 0.17 |
|  |  | 2-Naphthalenol, 1,2-dihydro-, acetate | N.D. | N.D. | N.D. | 0.17 | N.D. |
|  |  | Subtotal | 4.07 | 1.12 | N.D. | 1.04 | 0.22 |
|  | Ketones | 2-Nonadecanone | 0.71 | N.D. | N.D. | N.D. | N.D. |
|  |  | 2-Heptadecanone | 0.27 | N.D. | N.D. | N.D. | N.D. |
|  |  | Subtotal | 0.98 | N.D. | N.D. | N.D. | N.D. |
|  | Aldehydes | 2-Propenal, 3-phenyl- | N.D. | 0.07 | N.D. | N.D. | 0.04 |
|  |  | 3-Cyclopentene-1-acetaldehyde, 2-oxo- | N.D. | 0.06 | N.D. | N.D. | N.D. |
|  |  | Subtotal | N.D. | 0.13 | N.D. | N.D. | 0.04 |
|  | Oxides | 1-Methoxy-2-methyl-3-butene | N.D. | N.D. | 1.07 | N.D. | N.D. |
|  |  | 1-Butoxy-2-methyl-2-butene (E)- | N.D. | N.D. | 0.14 | N.D. | N.D. |
|  |  | Subtotal | N.D. | N.D. | 1.21 | N.D. | N.D. |
|  |  | Total | 17.92 | 11.20 | 6.79 | 5.95 | 5.36 |

Table S4. Effect of CFP temperature on the compound distribution in bio-oil (WTP temperature = 220 ºC, catalyst-to-biomass mass ratio = 3:1, catalyst = HZSM-5 (25))

| Substance | Category | Compounds | Absolute peak area (x107 a.u./mg) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 450℃ | 550℃ | 650℃ | 750℃ | 850℃ |
| Aromatics | MAHs | Benzene | 2.30 | 2.95 | 1.96 | 3.27 | 3.34 |
|  |  | Toluene | 1.52 | 2.60 | 2.86 | 5.24 | 6.50 |
|  |  | Xylene | 3.53 | 4.13 | 6.45 | 5.91 | 6.43 |
|  |  | Benzene, 1-ethyl-3-methyl- | 0.74 | 0.27 | 0.08 | 0.68 | 0.70 |
|  |  | Benzene, 1,2,3-trimethyl- | N.D. | N.D. | 0.09 | 0.69 | 0.20 |
|  |  | Benzene, 1-ethenyl-3-methyl- | N.D. | N.D. | N.D. | N.D. | 0.54 |
|  |  | Benzene, 1-methyl-4-(2-propenyl)- | 0.49 | N.D. | N.D. | N.D. | 0.21 |
|  |  | Benzene, 1-propenyl- | N.D. | 2.73 | 4.37 | 2.01 | N.D. |
|  |  | 3-Methylphenylacetylene | N.D. | N.D. | N.D. | N.D. | 0.97 |
|  |  | Naphthalene, 1,2-dihydro- | N.D. | N.D. | N.D. | 0.13 | 0.72 |
|  |  | Naphthalene, 1,2-dihydro-3-methyl- | N.D. | N.D. | N.D. | N.D. | 0.19 |
|  |  | 1H-Indene, 3-methyl- | 4.18 | 2.08 | 0.19 | 0.34 | N.D. |
|  |  | Subtotal | 12.77 | 14.77 | 16.02 | 18.27 | 19.90 |
|  | PAHs | Naphthalene | 2.56 | 2.22 | 3.74 | 3.02 | 1.50 |
|  |  | Naphthalene, 1-methyl- | 4.97 | 2.15 | 2.27 | 2.03 | 2.66 |
|  |  | Naphthalene, 2-ethyl- | N.D. | N.D. | N.D. | N.D. | 0.09 |
|  |  | Naphthalene, 1,3-dimethyl- | N.D. | 0.73 | 0.45 | 0.46 | 0.67 |
|  |  | Biphenyl | N.D. | N.D. | N.D. | 0.04 | N.D. |
|  |  | Naphthalene, 1,6,7-trimethyl- | N.D. | N.D. | N.D. | 0.10 | N.D. |
|  |  | Fluorene | N.D. | N.D. | N.D. | N.D. | 0.13 |
|  |  | Phenanthrene | N.D. | 1.96 | N.D. | 0.17 | 0.36 |
|  |  | Phenanthrene, 1-methyl- | N.D. | 0.13 | 0.07 | N.D. | N.D. |
|  |  | Anthracene | N.D. | N.D. | 0.12 | N.D. | N.D. |
|  |  | 1H-Cyclopropa[l]phenanthrene,1a,9b-dihydro- | N.D. | N.D. | N.D. | 0.09 | 0.18 |
|  |  | Subtotal | 7.53 | 7.19 | 6.65 | 5.96 | 5.57 |
|  |  | Total | 20.30 | 21.95 | 22.67 | 24.22 | 25.46 |
| Aliphatics | Alkanes | Cyclopropane, 1,2-dimethyl-, trans- | N.D. | N.D. | N.D. | 0.95 | N.D. |
|  |  | Heptacosane | 1.79 | 0.20 | 0.06 | N.D. | 1.62 |
|  |  | Octacosane | N.D. | 0.26 | 1.25 | N.D. | 0.62 |
|  |  | Subtotal | 1.79 | 0.46 | 1.31 | 0.95 | 2.24 |
|  | Olefins | 2-Butene | N.D. | N.D. | N.D. | N.D. | 0.59 |
|  |  | 1,4-Pentadiene | N.D. | 0.25 | 0.37 | 0.43 | N.D. |
|  |  | 1,2-Butadiene | N.D. | N.D. | N.D. | 0.43 | N.D. |
|  |  | 1,3-Cyclopentadiene | N.D. | N.D. | N.D. | 0.12 | 0.74 |
|  |  | 1,3,5-Hexatriene | N.D. | N.D. | N.D. | 0.50 | 0.62 |
|  |  | 2-Hexene, (Z)- | N.D. | N.D. | 0.11 | N.D. | N.D. |
|  |  | Bicyclo[4.2.0]octa-1,3,5-triene | N.D. | N.D. | 0.16 | 0.24 | 0.14 |
|  |  | 3-Methylphenylacetylene | N.D. | N.D. | N.D. | 0.73 | N.D. |
|  |  | D-Limonene | 0.08 | 0.11 | 0.09 | N.D. | 0.08 |
|  |  | Squalene | 4.70 | 5.85 | 5.43 | N.D. | 3.56 |
|  |  | Subtotal | 4.78 | 6.21 | 6.16 | 6.44 | 5.73 |
|  |  | Total | 6.57 | 6.67 | 7.47 | 7.39 | 7.97 |
| Oxygenates | Acids | Tetradecanoic acid | 0.28 | 0.38 | 0.13 | N.D. | N.D. |
|  |  | Pentadecanoic acid | N.D. | N.D. | 0.05 | N.D. | N.D. |
|  |  | Undecanoic acid | N.D. | N.D. | 0.04 | 0.16 | N.D. |
|  |  | Eicosanoic acid | N.D. | N.D. | N.D. | 0.05 | N.D. |
|  |  | 3,5-Dimethoxy-4-hydroxyphenylacetic acid | 0.09 | 0.09 | N.D. | N.D. | N.D. |
|  |  | Pentadecanoic acid | 0.24 | 0.86 | N.D. | N.D. | N.D. |
|  |  | 9-Hexadecenoic acid | N.D. | N.D. | 0.34 | 0.24 | 0.10 |
|  |  | Palmitoleic acid | 0.67 | N.D. | N.D. | N.D. | N.D. |
|  |  | n-Hexadecanoic acid | 5.89 | 5.75 | 4.32 | 1.22 | 1.99 |
|  |  | Heptadecanoic acid | N.D. | N.D. | N.D. | 0.80 | N.D. |
|  |  | Oleic Acid | 0.92 | 1.45 | 0.93 | 0.30 | 0.17 |
|  |  | Octadecanoic acid | 5.10 | 5.41 | 4.67 | 2.00 | 0.67 |
|  |  | Subtotal | 13.65 | 12.06 | 10.48 | 4.78 | 2.94 |
|  | Alcohols | 3-Buten-1-ol, 2-methyl- | 0.13 | 0.24 | 0.27 | N.D. | N.D. |
|  |  | 3-Cyclopentene-1,2-diol, cis- | 0.08 | N.D. | N.D. | 0.66 | N.D. |
|  |  | 1-Butanol, 2-methyl- | N.D. | N.D. | N.D. | N.D. | 0.07 |
|  |  | 4-Penten-1-ol | 0.14 | N.D. | N.D. | N.D. | 0.82 |
|  |  | 4-Methoxybenzene-1,2-diol | 0.09 | 0.26 | N.D. | N.D. | N.D. |
|  |  | 1-Tetradecanol | N.D. | N.D. | 0.12 | 0.30 | N.D. |
|  |  | Ethanol, 2-(octadecyloxy)- | N.D. | 0.15 | 0.15 | 0.65 | 0.36 |
|  |  | 1-Heptatriacotanol | N.D. | N.D. | N.D. | N.D. | 0.18 |
|  |  | Subtotal | 0.44 | 0.64 | 0.54 | 1.60 | 1.43 |
|  | Esters | Hexadecanoic acid, methyl ester | 0.25 | 0.16 | 0.12 | N.D. | N.D. |
|  |  | Methyl stearate | 0.45 | 0.34 | N.D. | N.D. | N.D. |
|  |  | Hexadecanoic acid, 2-(octadecyloxy)ethyl ester | 0.48 | N.D. | 0.11 | 0.03 | N.D. |
|  |  | Oleic acid, 3-(octadecyloxy)propyl ester | N.D. | 0.11 | 0.11 | 0.21 | 1.13 |
|  |  | Subtotal | 1.18 | 0.61 | 0.35 | 0.25 | 1.13 |
|  | Furans | Furan, 2-methyl- | 0.06 | 0.13 | 0.12 | 0.14 | 0.43 |
|  |  | 3-Methyl-2-(2-methyl-2-butenyl)-furan | 0.21 | 0.16 | 0.08 | 0.02 | N.D. |
|  |  | Benzofuran, 2,3-dihydro- | 0.42 | 0.34 | 0.31 | 0.24 | N.D. |
|  |  | Subtotal | 0.69 | 0.63 | 0.51 | 0.40 | 0.43 |
|  | Phenols | Creosol | 0.28 | 0.22 | N.D. | N.D. | N.D. |
|  |  | Phenol | N.D. | 0.09 | 0.27 | 0.45 | N.D. |
|  |  | Phenol, 4-ethyl-2-methoxy- | 0.09 | 0.36 | 0.32 | 0.67 | N.D. |
|  |  | p-Cresol | N.D. | 0.21 | 0.39 | 0.44 | N.D. |
|  |  | Phenol, 2,6-dimethoxy- | 0.60 | 0.38 | 0.29 | 0.17 | N.D. |
|  |  | 1-Naphthalenol, 1,2,3,4-tetrahydro-3-methyl- | N.D. | N.D. | N.D. | 0.11 | N.D. |
|  |  | 1-Naphthalenol | N.D. | N.D. | N.D. | 0.07 | N.D. |
|  |  | (E)-2,6-Dimethoxy-4-(prop-1-en-1-yl)phenol | 0.15 | 0.11 | N.D. | N.D. | N.D. |
|  |  | Subtotal | 1.12 | 1.37 | 1.27 | 1.91 | N.D. |
|  | Ketones | Ethanone, 1-(1-cyclohexen-1-yl)- | N.D. | N.D. | 0.09 | N.D. | N.D. |
|  |  | Subtotal | N.D. | N.D. | 0.09 | N.D. | N.D. |
|  | Aldehydes | Furfural | 0.12 | N.D. | N.D. | N.D. | N.D. |
|  |  | 2-Propenal, 3-phenyl- | N.D. | N.D. | N.D. | 0.18 | N.D. |
|  |  | Subtotal | 0.12 | N.D. | N.D. | 0.18 | N.D. |
|  | Oxides | 1-Butoxy-2-methyl-2-butene (E)- | N.D. | N.D. | N.D. | N.D. | 0.14 |
|  |  | 3,5-Dimethoxy-4-hydroxytoluene | 0.78 | N.D. | N.D. | N.D. | N.D. |
|  |  | 1-Methoxy-2-methyl-3-butene | N.D. | N.D. | N.D. | N.D. | 1.07 |
|  |  | D-Allose | 0.44 | 1.05 | 0.31 | 0.22 | N.D. |
|  |  | Subtotal | 1.22 | 1.05 | 0.31 | 0.22 | 1.21 |
|  |  | Total | 18.46 | 16.53 | 13.58 | 9.43 | 6.79 |